## Slide 1
Mixture system
Double checking the equal-pressure, equal-temperature mixing solutions derived by Philip
Exploring potential scaling law for cold curves generated for a series of elements by the LLNL Purgatorio code
Single phase

## Slide 3
Free energy modeling of a single phase

## Slide 4: Standard decomposition of free energy

## Slide 5: Other functions derived from free energy

## Slide 7: Multiphase construction
Multi-Phase Approach
Construct free energy for each phase
Maxwell construction  Phase transition
… for each isotherm
FA(VA) - FB(VB) = - P (VB - VA)
“Flattened”
= NO metastable
extensions

## Slide 8: Cold Curve: Beyond Analytical Functions
One example of Be hcp cold curve
EXP
DFT
Vinet
B1 does not change
Breakpoint
Soft-sphere model
Traditional treatment of cold curve: using analytical functions

## Slide 9
curvallis.py --input Pc_hcp.dat --back Pc_hcp.dat --region_data_points 15 --x_max 8

## Slide 10
Ag/ Ar/ Au/ Bi/ Cl/ Cr/ D/ Fe/ Ga/ H/ Kr/ Mg/ Mo/ Ne/ Pb/ Po/ Re/ S/ Sn/ T/ Ti/ Y/ Zr/
Al/ As/ Be/ Ce/ Co/ Cu/ F/ Fr/ Ge/ He/ Li/ Mn/ N/ Os/ Pd/ Pt/ Rh/ Se/ Sr/ Ta/ Xe/ Zn/
H

## Slide 11
Scaling for TF table: